MIPOLAM AFFINITY

MIPOLAM AFFINITY is a vinyl flooring homogeneous pressed in 2m sheets, with a thickness of 2mm and a weight of 2800g. The non-directional design with colour throughout the thickness is available in 50 references presenting a contrasted designed & a matt finish.

This flooring is recommended for collective buildings making skirtings easier, as well as angles and welding.

The flooring is equipped with Evercare ™, patented surface treatment obtained by UV laser cross-linking offering the best chemical resistance to the main products used in healthcare environment as betadine, eosin, hydro alcoholic solutions, making the maintenance easy and the floor long lasting. This treatment avoids applying any acrylic emulsion throughout the lifetime of the product.

It is free of formaldehyde, heavy metals and CMR 1 & 2 or vPvB (very persistent and very bio  accumulative) or PBT (persistent, bio-accumulative and toxic) and is REACH compliant. It is 100% phthalates free and recyclable.
Its VOC emissions after 28 days (ISO 16000-6) are below detection levels (<10 μg / m3) and this product is classified A + (the best class).

According to ISO 21702, Mipolam Affinity has anti-viral activity against Human Coronaviruses : it reduces the number of virus by 99,7% after 2h00.

According to ISO 22196, Mipolam Affinity has anti-bacterial activity againt E. coli, S. aureus and  MRSA of 99% after 24h00.

This flooring is antistatic (<2kV), its residual indentation is ≤ 0.02 mm to 150 minutes respecting EN ISO 24343-1 (EN 433).

This flooring complies with EN ISO 10581 offering a Binder content Type I, which makes it suitable for heavy duty traffic areas.
It has a Bfl-s1 fire resistance.