MIPOLAM EVO

MIPOLAM EVO™ is a new generation of resilient flooring, made with a patented blend of synthetic thermoplastic polymers. It is a fully flexible homogeneous compacted floorcovering, available in sheet, 2m wide. It provides providing excellent resistance to wear and tear in high traffic areas. Its weight is 2700 gr/m².

Its composition is 100% REACH compliant ; it contains no PVC and no plasticizer.

The product ensures perfect indoor air quality (TVOC <10 microgramms / m3 after 28 days according to NF EN16000-6)) and is Floorscore and Blue Angel certified.

It features 14 colours based on a timeless design with colours throughout its thickness presenting a nice matt finish.

The flooring is equipped with Evercare ™, patented surface treatment obtained by UV laser cross-linking offering the best chemical resistance to the main products used in healthcare environment, such as betadine, eosin, hydro alcoholic solutions, making the maintenance and disinfection easy and long lasting.

This treatment avoids applying any acrylic emulsion throughout the lifetime of the product.

The flooring is antistatic (<2kV), its residual indentation is ≈ 0.02 mm.

The flooring complies with the EN ISO 19322 norm, has a binder content Type I and is suitable for heavy duty traffic areas.

It is Bfl-s1 fire resistant and is rated R10 for antislip resistance.

It is 100% recyclable. 100% of their post manufacturing waste get recycled.

As thermoplastics, its recycled content replaces virgin material and is on average 20%.

Designed and manufactured in a sustainable way in a plant awarded with ISO 9001 (quality), ISO 14001 (environment) and ISO 50001 (energy) certifications, the flooring is certified Cradle to Cradle™ Silver.

According to ISO 21702, Mipolam Evo has anti viral activity against Human Coronaviruses : it reduces the number of virus by 99,7% after 2h00.

According to ISO 22196, Mipolam Evo has anti bacterial activity against E. coli, S. aureus and  MRSA of 99% after 24h00.