GTI PURE connect

GTI PURE CONNECT is a multi-layered interlocking loose lay vinyl tile with polyurethane treatment (PUR+), 6 mm thick with a dovetail joint, abrasion group T. It is manufactured by GERFLOR using a continuous and exclusive high pressure process.

The GTI PURE CONNECT wear layer is a pure vinyl homogeneous wear layer with no filler, incorporating very densely pressed coloured chips and without a transparent wear layer that offers an outstanding abrasion and scratch resistance and an high resistance to traffic.

GTI PURE CONNECT is reinforced with 2 glass fiber grids on either side of an intermediate pressed homogeneous layer.

GTI PURE’s backing is a 5 mm thick black pressed homogeneous sheet, its surface is a colored and reinforced homogeneous sheet 1 mm thick.

It is made of 100% controlled recycled materials.

It is 100% recyclable and made with up to 80% recycled content.