#

**CREATION 40 ZEN** is an acoustic and decorative floor, in PVC multilayers reinforced with a fiber veil, available in tile and plank format, with 4 beveled edges.

It has antistatic abrasion group T, and R10 antislip performance.

Theoverall thickness is 3.60 mm, and the product has 0.40 mm transparent wearlayer.

**The high density foam** provides **good indentation resistance** of 0.12 mm (average mesure) and **high acoustic insulation level** (-20 dB)

It benefits from a cross-linked polyurethane surface treatment (ProtecshieldTM), making maintenance easier and prevent from micro scratches.

**CREATION 40 ZEN** has a European class (residential / commercial) 23/32 according to EN-ISO 10874 and has Bfl-s1 class for smoke emission according to EN 13501-1.

**CREATION 40 ZEN is a looselay product,** maintained with tackifier**.**

This installation allows, among other things, an installation on asbestos-contaminated support, and is removable

**CREATION 40 ZEN** is made with phthalate free plasticizers. It is 100% recyclable and 100% compliant with REACH. The product emission rate of organic compounds is < 10µg/m3 (TVOC <28 days – ISO 16000-6).

**CREATION 40 ZEN** is made in France