#

**CREATION 70 ZEN** is an acoustic and decorative floor, in PVC multilayers reinforced with 2 fiber glass layers, available in tile and plank format, with 4 beveled edges. It has an antistatic abrasion group T, and R10 antislip performance.

It consists in a 0.70 mm thick transparent wear layer, the overall thickness is 4.35 mm.

**The high density foam** provides good **indentation resistance** of 0.12 mm. (average mesure) and **high acoustic insulation level** (-20dB).

Thanks to its double reinforcement, **fiber veil + fiber grid**, and to a **calendared intermediate layer** which gives it greater density, the coating retains its dimensional **stability** under the effect of a temperature variation (<0.03%).

It benefits from a cross-linked polyurethane surface treatment (ProtecshieldTM) for making maintenance easier and prevent from micro-scratches.

**CREATION 70 ZEN** is resistant to high traffic (commercial / industrial use) 34/42 according to EN-ISO 10874 and has Bfl-s1 class for smoke emission according to EN 13501-1

**CREATION 70 ZEN is a looselay product,** maintained with tackifier**.**

This installation allows, among other things, an installation on asbestos-contaminated support, and is removable.

**CREATION 70 ZEN** is **made in France** with **15% of recycled content** and **phthalate free** plasticizers (excepted recycled content). It is 100% recyclable and 100% compliant with REACH.

Its VOC emissions after 28 days (ISO 16000-6) are below detection levels (<10 μg / m3)

It has - according to the ISO 21702 - an anti-viral activity against the human Coronavirus, reducing the number of viruses by 99.7% after 2 hours.

It has antibacterial efficacy (E.coli / S.aureus / MRSA) : >99% after 24 hours according to ISO22196.