# MURAL REVELA is a rigid vinyl wall covering which has a thickness of 5mm for an extended durability. It is available in 2 formats of 65 x 37,5cm for tiles or 260 x 90cm / 260 x 120cm for panels.

# It is intended for indoor use.

# Its non-porous conception, its tongue and groove assembly system combined with a glued installation give MURAL REVELA a water resistance allowing an installation in wet areas including showers.

# Thanks to its robust conception and the total thickness of the product, MURAL REVELA is an ideal solution for renovation on ceramic tiles.

# It has a fire reaction classification D-s3,d0 according to EN13501.

# It has excellent chemical resistance according to EN 423.

# It will be CMR 1 & 2 free and 100% Reach compliant.

# TVOC 28-day air emissions (NF EN 16000-6) will be classified as A+ (best class) under French health labelling.

# MURAL REVELA has been designed and is produced in Europe.

# MURAL REVELA contains up to 30% recycled and is 100% recyclable. It can be collected and recycled through the Gerflor Second Life programme (selected countries).