MARMORETTE LCH is a calendered linoleum compact dissipative floorcovering in sheet, 2m wide, providing excellent resistance to everyday wear and tear in high traffic areas. Its vertical resistance is 1x10⁶ ≤ R ≤ 1x10⁸.

Its weight is 3000g/sqm in 2.5mm.

It features a marbled design and presents a matt finish, is composed of 98% natural materials (bio-based and mineral): linseed oil, wood flour, resins, cork, minerals and jute fabric, among which 76% are rapidly renewable.

The flooring is equipped with Neocare surface treatment, making the maintenance easy and the flooring long lasting.

The flooring is 100% recyclable, is composed of minimum 25% recycled content and up to 40% recycled content, 100% controlled, is REACH compliant and rated Cfl-s1 for fire resistance.

It is designed and manufactured in a sustainable way in a plant awarded with ISO 9001 (quality), ISO 14001 (environment) and ISO 50001 (energy) certifications.

The Camouflage welding rod makes the connections between the strips invisible.

It is antistatic, antibacterial according to ISO 22196 / JIS Z 2801.

For environments where dissipative properties are required.

Made of 98% natural (bio based and mineral) and 76% rapidly renewable materials

Up to 40% recycled content

Blue Angel and Floorscore certified

Exclusive Neocare™ surface treatment : best in class micro scratch and stain resistance, easy maintenance, no emissions

Hygienic properties : antibacterial activity (EN ISO 22196) and antiviral activity (ISO 21702)

Vertical Resistance (EN 1081): 1x10⁶ ≤ R ≤ 1x10⁸.