CREATION 55 LOOSELAY ACOUSTIC is a synthetic, decorative, flexible, antistatic, abrasion group T floorcoverings available in tiles and planks with beveled edges. It consists in a 0,55 mm thick transparent wear layer, a design film and a double calandered layer reinforced with a fiber glass veil. The backing integrates an acoustic foam reaching 19dB acoustic impact noise reduction. The overall thickness is 5.5 mm.

They benefit from a cross-linked polyurethane surface treatment (Protecshield), making maintenance easier and eliminating the need for initial polishes.

CREATION 55 LOOSELAY ACOUSTIC is a looselay floorcovering, resistant to use (commercial / industrial use) of 33 / 42 according to EN-ISO 10874 and has Bfl-s1 class for smoke emission according to EN 13501-1.

CREATION 55 LOOSELAY ACOUSTIC is made with phthalate free plasticizers, except recycled content. It is 100% recyclable and have up to 35% of recycled content. It is REACH compliant. The product emission rate of organic compounds is < 10µg/m3 (TVOC <28 days – ISO 16000-6).